Supporting Information

for

Probing the Interaction Mechanisms of Lipid Nanoparticle-Encapsulated mRNA with Surfaces of Diverse Functional Groups: Implication for mRNA Transport

Jingyi Wang†1,3, Jiawen Zhang†2,3, Sijia Li3, Hui Qian4, Dengfeng Liu5, Isaias Prado5, Sharon Wang5, Akhilesh Bhambhani5, Hongbo Zeng3,*

1. College of Chemistry and Chemical Engineering, Southwest Petroleum University, Chengdu, Sichuan, 610500, China

2. School of Materials Science and Engineering, Southeast University, Nanjing 211189, China

3. Department of Chemical and Materials Engineering, University of Alberta, Edmonton, AB, T6G 1H9, Canada

4. Nanotechnology Research Center, National Research Council Canada, Edmonton, AB T6G 2M9, Canada

5. Ultragenyx Pharmaceutical Inc., 5000 Marina Blvd, Brisbane, CA 94005, USA

*Corresponding author. E-mail: hongbo.zeng@ualberta.ca (H. Zeng), Phone: +1-780-492-1044

† J. Wang and J. Zhang contributed equally to this work

Figure S1. Water contact angle on thiol-functionalized gold surface.

Figure S2. XPS spectra of gold surface functionalized with HS(CH2)10COOH.

Figure S3. XPS spectra of gold surface functionalized with HS(CH2)10CH2OH.

Figure S4. XPS spectra of gold surface functionalized with HS(CH2)10CH2NH2.

Figure S5. XPS spectra of gold surface functionalized with HS(CH2)10CH2PO3H2.

Figure S6. XPS spectra of gold surface functionalized with HS(CH2)10CH3.